RIE Quiz Question Finalization:

- This document is broken down into each of the 8 sections of the RIE module. Each has its own page.

- Question options are a combination of two documents, one I have previously shared, and one that Mohammed had provided in Teams. I have refactored all of his questions into a multiple-choice format found mixed in here. I have also removed a couple of my own questions that I felt were not at the same level of rigor/applicability as his questions.

Items To Be Addressed:

Underneath each of these items to be addressed, feel free to write:

[Your Name: Your thoughts, with references to a proposed quiz question which is denoted by Section (S)#, Question (Q)#]

- Are 3 quiz questions per section too much? If so, please indicate which question you think should be eliminated from each section besides section 4.

Olivia: I believe photolithography currently has 1-2 questions per section. All of the sections of this document have 3 except for section 4 (Loading the Wafer) which only has 2. I personally think 3 would be okay, but I would like to hear other opinions.

- There is a lack of low-rigor questions similar to the photolithography module where the user matches equipment names to their picture. Do we feel like we need some of these for this module?

Olivia: I am unsure how helpful those style questions were for the photolithography module since there is not very much equipment in that room. While I do think they would be more useful for this module since there is more equipment, I must then question our consistency in quiz difficulty across the modules if we elect to not include that question type in RIE. Should we not then add more conceptual, process-centric questions to the photolithography module?

- I am planning on presenting these questions in the order that they are numbered in this document. Please indicate if you think the order should be adjusted in any way.

- Any other comments/questions/concerns about the proposed quiz content?

SECTION 1)     Support Room Machine Startup

S1Q1:  What is a Reactive Ion Etching (RIE) system used for in microfabrication?

- To add material to a substrate using a liquid chemical bath.

- To remove material using a chemically reactive plasma in a vacuum chamber.

- To physically remove material with high-energy ions, but without chemical reactions.

- To clean silicon wafers using a solution of hydrofluoric acid.

Answer: B. RIE uses chemically reactive plasma within a vacuum environment to remove material from a substrate. It is a type of dry etching system.

S1Q2: Which of the following materials cannot be etched with RIE?

- Polymers

- Si

- SiO2

- Au

- Si3N

- GaAs

Answer: D. Au or Gold is chemically inert and doesn't form volatile compounds easily with common RIE gases (fluorine, chlorine, oxygen plasmas). It is typically removed by wet etching, not RIE.

S1Q3: T/F: To turn on the gas tanks, you rotate the valves in the clockwise direction.

Answer: False. The statement is backwards. You rotate the valves counterclockwise.

SECTION 2)      Front Room Machine Startup

S2Q1: Which of the following is NOT a part of the safety precautions for operating an RIE system?

- Use appropriate PPE (gloves, goggles, lab coat)

- Confirm gas line integrity and exhaust function before starting

- Understand the properties and hazards of process gases and chemicals before operation

- Modifying procedures as needed without authorization

- Understand and be familiar with emergency shutdown procedures

Answer: D

S2Q2: Which pair of etch gases and materials is unsuitable?

- Si: SF6 or CF4

- SiO2: CHF3 or CF4/O2

- Si3N4: CHF3/O2

- Metals (e.g.,Al): CL2/BCl3

- Quartz: Cl2/BCl3

- Photoresist: O2

Answer: E. Quartz is SiO2, which has a suitable pairing with CHF3 or CF4/O2

S2Q3: What temperature should the front-room chiller reach before you start using the computer to run the RIE machine?

- 20 C

- 21 C

- 22 C

- 23 C

- 24 C

Answer: A. 20 C

SECTION 3)     Pre-Load Software Steps

S3Q1: When reading the screen of the RIE, what does ATP and ACT refer to?

- ATP: Wafer Temperature, ACT: Chamber Temperature

- ATP: Machine Controller Temperature, ACT: Turbo Pump Temperature

- ATP: Machine Stage Temperature, ACT: Plasma Temperature

- ATP: Turbo Pump Temperature, ACT: Machine Controller Temperature

Answer: D. ATP: Turbo Pump Temperature, ACT: Machine Controller Temperature

S3Q2: T/F: You should monitor ATP and ACT values at all times.

Answer: True.

S3Q3: What is the purpose of evacuation?

- To introduce reactive gases for etching.

- To remove unwanted gases and contaminants.

- To cool down the wafer during the etching process

- To increase the etch rate and anisotropy.

- To enable high-pressure plasma generation.

Answer: B. Evacuation removes unwanted gases and creates a low-pressure environment for plasma generation.

SECTION 4)      Loading the Wafer

S4Q1: In Reactive-Ion Etching (RIE), which sequence correctly describes how material is removed from a substrate?

- Introduce reactive gas > Apply radio frequency (RF) power to create plasma > Ions react and sputter material > Pump out volatile byproducts.

- Substrate in chamber > Introduce wet etchant > Chemical reaction occurs > Byproducts dissolve.

- Substrate in chamber > Ions physically etch > Byproducts desorb > Vacuum pump removes.

- Apply heat to substrate > Sublimation > Vapor removed > Surface etched

- Introduce inert gas > Apply DC voltage to create plasma > Electrons bombard to remove material > Neutralize charged byproducts with counter-ions.

Answer: A

S4Q2: How do you open the RIE chamber lid?

- Press one of the hoist buttons.

- Turn the switch to chamber up, and it will open automatically.

- Turn the switch to chamber up, and press one of the hoist buttons.

- Turn the switch to chamber up, then press and hold both of the hoist buttons.

- Turn the switch to chamber up and press both of the hoist buttons.

Answer: D

SECTION 5)      Etching and Running the Recipe

S5Q1: T/F: You should never change the gas concentrations before running a recipe.

Answer: False. You should always check the flow rate, process time, and power values before running a recipe and adjust them if needed.

S5Q2: Why is plasma necessary during Reactive Ion Etching? Plasma...

- Acts as a heat source to melt and remove the material.

- Provides UV radiation to solidify the patterned mask.

- Generates reactive ions and radicals that chemically react with the material and physically sputter it away.

- Creates a vacuum that draws material away from the substrate.

- Forms a protective layer to prevent etching of the substrate.

Answer: C. Ions bombard the surface, physically removing the material and enchancing the vertical etch directionality (anisotropy).

S5Q3: Which is NOT a key parameter in a standard RIE process?

- RF power

- Evacuation duration

- Chamber pressure

- Gas type and its corresponding flow rate

- Etch time

Answer: B, Evacuation Duration.

SECTION 6)      Removing the Wafer

S6Q1: T/F: It is impossible to see a difference in the sample’s appearance after etching without the use of a microscope.

Answer: False

S6Q2: You must wait for the turbo pump to reach 0 RPM before exiting service mode on the computer.

Answer: True

S6Q3: After using profilometry, ellipsometry, or SEM to measure thickness before and after etching, how is etch rate calculated?

- Etch Rate = Time / (Initial + Final Thickness)

- Etch Rate = (Final – Initial Thickness) / Time

- Etch Rate = (Initial – Final Thickness) / Time

- Etch Rate = (Initial + Final Thickness) / Time

- Etch Rate = Time / (Initial – Final Thickness)

Answer: C, Etch Rate = (Initial – Final Thickness) / Time

SECTION 7)      Front Room Machine Shutdown

S7Q1: Which of the following does NOT cause non-uniform etching across the wafer?

- Poor gas distribution

- Inconsistent electrode contact or RF power distribution

- Chamber loading effects

- Excessive etching time, leading to over-etching

- Stable chamber pressure

Answer: E. Maintaining a stable and optimized chamber pressure is crucial for uniform etching.

S7Q2: How can a small area be etched on a wafer using the RIE system?

- By submerging the wafer in a liquid chemical.

- By applying a broad plasma etching process to the entire wafer.

- By creating a mask that exposes only the specific area to etch.

- By using a laser to burn away unwanted material.

- By physically scraping away the unwanted material.

Answer: C. By creating a mask that exposes only the specific area to etch.

S7Q3 T/F: The small chiller automatically turns off when you press the red power “OFF” button on the RIE machine.

Answer: True

SECTION 8)      Support Room Machine Shutdown

S8Q1: T/F: When shutting down the support room machine, you turn them off in the exact same order that you turned them on.

Answer: False. You turn them off in the exact opposite direction.

S8Q2: T/F: In commercial settings, it is likely that gases will remain on all day.

Answer: True

S8Q3: How frequently should the chamber of the RIE be cleaned and maintained?

- After every single etching process, regardless of type.

- Only when noticeable malfunctions or performance drops occur.

- Weekly or following heavy polymer-forming processes.

- Monthly, using only dummy wafers for all cleaning steps.

- Yearly, with only visual inspection of the chamber components.

Answer: C. Weekly or after heavy polymer-forming processes. Dummy wafers or O2 plasma should be used to clean. Electrodes and gaskets should be inspected regularly